## Slide 1: Cp-T-Fit.py
Purpose: Analyze Debye temperature by fitting Cp–T data
Model: Debye model
Functions: (i) mode = ‘sim’: Plot Cp – T and TD – T data to estimate the Debye temperature TD (iii) mode = ‘fit’: Non-linear least-squares fitting to Debye model
Theory: Attached in this file after usage of the program

## Slide 2: Estimate Debye temperature from Cp/Cv – T data
Program: [data-COE]\Cp\Cp-T-Fit.py
[Programs]\python\Cp\Cp-T-Fit.py
データ: [data-COE]\Cp
Usage:
python Cp-T-Fit.py mode infile ciffile args
(i) python Cp-T-Fit.py infile(.xlsx) ciffile TD Cp0
ex: python Cp-T-Fit.py sim Ba3SiO-heat capacity.xlsx Ba3SiO-11.cif
(ii) python Cp-T-Fit.py infile(.xlsx) ciffile TD optid(TD) Cp0 optid(Cp0)
ex: python Cp-T-Fit.py fit Ba3SiO-heat capacity.xlsx Ba3SiO-11.cif 300.0 1
Input files: Excel (.xlsx)
CIF file (.cif)
parameter file (.in)
Output files: parameter file (.in)
CSV files

## Slide 3: Input file: Excel
SrTiO3-Cp .xls
The first and second columns must be temperature T [K] and heat capacitance [J/K/g]
T(K) | Cp (J/K/g)
303.101 | 0.55365
303.2 | 0.55376
303.299 | 0.55385
303.398 | 0.55397
303.496 | 0.55406
303.594 | 0.55415
303.694 | 0.55423
303.793 | 0.55434
303.892 | 0.55444
303.992 | 0.55453
Input file: CIF
CIF file is used to aculate number density of atoms and the Dulong-Putit limit

## Slide 4: 1st step: Estimate Cp0 and TD (Debye temperature)
python Cp-T-Fit.py sim SrTiO3-Cp.xlsx SrTiO3.cif
Console output:
Atom density : 8.39667e+22 cm^-3
0.0272484 mol/g
Dulong-Putit limit: 24.9435 J/K/mol
0.679671 J/K/g
Cp(max): 0.6691 J/K/g
# Maximum value in the measured Cp
Cp lower limit for TD approximation: 0.02409 J/K/g
# The approximation eq is valid for the measured Cp data larger than this value
Estimate TD
From plateau
600 K or 450 K?

## Slide 5: 2nd step: Simulate with estimated TD
python Cp-T-Fit.py sim SrTiO3-Cp.xlsx SrTiO3.cif 600
python Cp-T-Fit.py sim SrTiO3-Cp.xlsx SrTiO3.cif 450

## Slide 6: Parameter file: *.in
Parameter file is stored with mode = ‘sim’
SrTiO3-Cp.in
[Parameters]
TD=602.2871861768992:1 # value:optid if optid = 0 the parameter is not optimized
Cp0=0.6796706010351087:1
[Configuration]
Tfitmin=0.0 # Edit if you want to limit fitting T range
Tfitmax=0.0 # Edit if you want to limit fitting T range
Cpmax=0.66912

## Slide 7: 3nd step: Fitting
python Cp-T-Fit.py fit SrTiO3-Cp.xlsx SrTiO3.cif
Cp, TD, and other configurations are read from SrTiO3-Cp.in No extra arguments are not needed.
Console output:
Optimized at S2= 9.93373e-05:
TD : 579.18094 optid=1
Cp0 : 0.38041057 optid=1
Initial
Optimized

## Slide 8: Final step: Check over wide T range
python Cp-T-Fit.py sim SrTiO3-Cp.xlsx SrTiO3.cif
Cp, TD, and other configurations are read from SrTiO3-Cp.in

## Slide 9: Theory

## Slide 10: Debye model
Consider all atomic vibrations are acoustic modes with the phonon density of states of for .
Replacing by
[J/K/mol]
: Debye temperature
: Debye function
High-T limit:
Low-T limit:
Dulong-Putit law
python debye_function.py 300 0 500 10
calculate Debye function with
Debye T 300K T range 0 – 500 K, 10 K step

## Slide 11: Approximate evaluation of
[1] Lei Feng, et al 2015 Appl. Phys. Express 8 071501
[2] G. Burns, Solid State Commun. 35, 811 (1980).
[3] A. Duran, et al. J. Phys.: Condens. Matter 20, 085219 (2008).
Debye Temperature (K) |  |  | 
Cal. |  | Exp. | 
731.5[1] (LDA) | 627.4[1] (GGA) | 633[2] | 640[3]

## Slide 12: §5.2 固体の比熱: 古典統計 (アインシュタイン模型)
P. 103 (阿部龍蔵「統計力学」 裳華房)
格子振動の Einsteinモデル
・ 固体中の原子が一次元に独立に振動していると近似
・ 調和振動子
(5.13)
分配関数 f
(5.14)
まずは古典統計 （Maxwell-Boltzmann分布) で考える
運動エネルギー、ポテンシャルエネルギーの それぞれの自由度に kBT/2 が分配されている: エネルギーの等分配則
デュロンープティの法則 固体の比熱は、構成元素の種類、温度に依存せず一定 ~25 J/(molK)
・ 室温で実測に良く一致
・ 熱力学第三法則と矛盾 T  0 で S  
・ 実測は低温で CV は減少、T  0 で CV  0
定積モル比熱の定義より (3次元の振動では、平均エネルギーは(5.14)式の3倍)
(5.21,22)

## Slide 13: 比熱のアインシュタイン模型
量子力学の調和振動子モデル： 1自由度に のエネルギーを持つフォノンが n個 零点エネルギー /2 が付随
1自由度の調和振動子の平均エネルギー: Planck分布 ＋ 零点エネルギー
定積モル比熱の定義より
・ T >> (=  0) で
デュロンープティの法則
・ T  0 ( >> 1)で
であり、CV は 1/T に対して指数関数的に減少する。
・ 熱力学第三法則との矛盾は解消された
・ 残っている問題： 実験的に、固体の比熱は低温では T 3 に比例する

## Slide 14: §9. デバイ模型におけるフォノンの状態密度
P. 196
状態密度 g(E) 便宜的に、1辺の長さ L の立方体による周期境界条件を考える。
可能な波長は、 , , を整数として
, ,
、波数 については以下となる。
,, (9.5)
1つの n = (nx, ny, nz) に対して  が決まり、一つの調和振動子が対応する。
1つの調和振動子が占める k空間での体積 vk は (9.5)式から
(9.6)
k空間の微小体積 dk 中の状態数は dk
|k| ~ |k| + dk の範囲にある状態数は、この体積素片の関係 dk = 4k2dk から、
(9.7)
(9.4)式  = slk (d = sl dk) を使って変数を k   に変換する。
)d (9.8)
これが、 ~  + d の範囲にある状態数であり、
g() を「 に関する 状態密度」という。

## Slide 15: §9. デバイ模型におけるフォノンの状態密度
P. 196
横波は2つあるので、全状態密度は st を 横波の音速として
(9.9)
(9.12)
連続的な弾性体の音波ではなく、原子の連成振動として
正しく波動方程式を解けば、格子間隔より短い波長の波はありえない
=>  には上限 D がある
原子数を N とすると格子振動の自由度は 3N
(9.13)
フォノン状態密度

## Slide 16: §9. 理想ボース気体: デバイ模型
P. 195
量子力学の調和振動子モデル： 角振動数  の調和振動子のエネルギー
フォノン 1つが エネルギー をもつ
Planck分布から、この調和振動子のエネルギーの統計平均は
(9.17)
(9.18)
とおくと、
(9.19)
エネルギーを表すのに、温度で表すとわかりやすい
(9.20)
: Debye温度 多くの物質では数百K 程度

## Slide 17: §9. デバイ模型の比熱: 高温
P. 201
エネルギーを表すのに、温度で表すとわかりやすい
D: Debye温度 多くの物質では数百K 程度
(9.20)
(9.21)
高温の場合: D / T, x << 1 (以下、零点エネルギーは無視する)
(9.22)
(9.23)
(9.24)
デュロンープティの法則

## Slide 18: §9. デバイ模型の比熱: 低温
P. 202
(9.21)
低温の場合: D/T, x >> 1、積分の上限 D/T を と近似できる
公式
(9.25)
(9.26)
(9.27)
Einstein模型では説明できなかった
低温での T 3 則を説明できる

## Slide 19: §9. デバイ模型の比熱: 全温度領域
P. 203
(9.21)
一般の場合
Debyeの比熱式
(9.29)
(9.30a)
(9.30b)
Debye関数
, y  0 で fD(y)  1 (デュロンープティの法則)
Alの比熱
実線は D = 396 K

## Slide 20
  金属の電子比熱 (8.67)
  (8.54, 8.65)
  格子比熱 (9.27)
  => (8.68)
  (8.69)
  とし、直線の切片と傾きから と を決定する
有効質量と音速
P. 185
８－５図
と の関係
  有効質量 ：
  音速の平均 :
Ref.Y. Xiao et al., Phys.Rev.. B 94, 125203 (2016)